- DocumentNo.: UPM-Nb2O5-001
Revision: V1.0
Issue Date: 2026-08-05

TECHNICAL DATA SHEET echnical Data Sheet

UltraPurMat Group Co., Ltd

Niobium Pentoxide Rotary Target

- Product Introduction

- Niobium Pentoxide (Nb2O5) Rotary Target is a high-purity ceramic sputtering material with a stable oxide structure and excellent chemical stability. It features high temperature resistance, good optical properties, and stable thin film deposition performance. Designed for magnetron sputtering applications, Nb2O5 rotary targets are widely used in optical coatings, semiconductor thin films, display technologies, and advanced research applications.

- Product Characteristics

- High purity ceramic material with excellent compositional uniformity and low impurity content

- Excellent chemical stability, thermal stability, and resistance to high-temperature sputtering environments

- Stable sputtering performance with uniform film deposition for optical and functional thin film applications

- High refractive index and excellent optical properties, suitable for advanced coating applications

- Available in customized rotary target dimensions for different magnetron sputtering systems

- Product Specifications

| - Product ID | - Formula | - Purity | - Size |
| --- | --- | --- | --- |
| - 410800RT001 | - Nb2O5 | - 99.9% | - ID125mm x OD133mm x 850mm |
| - 410800RT002 | - Nb2O5 | - 99.95% | - OD32 mm x ID23 mm x 150mm |
| - 410800RTC01 | - Nb2O5 | - Customized | - Customized |

| - Chemical Compositions (ppm) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| - Purity | - Ta | - Si | - Fe | - Cu | - Al | - Sn | - W |
| - 99.9% | - ≤80 | - ≤80 | - ≤80 | - ≤30 | - ≤20 | - ≤10 | - ≤30 |
| - 99.99% | - ＜10 | - ＜10 | - ＜5 | - ＜5 | - ＜5 | - ＜5 | - ＜5 |

- Typical Physical Properties

| - Parameter | - Specification |
| --- | --- |
| - Density | - ≥ 4.7g/cm3 |
| - Resistivity | - < 50mΩ·cm |
| - Roughness | - ≤ 3.2μm |

- Typical Applications

- Niobium Pentoxide (Nb2O5) Rotary Target is widely used in optical coating materials, semiconductor thin films, display coatings, and advanced sputtering applications.

- Packaging

- Outer Packaging: Wooden Crate

- Inner Packaging: Double-layer Vacuum-sealed Bag.

- Packaging Specifications: 1 piece/box.

- Custom packaging available upon request.

- Storage

- During transportation and storage, avoid moisture, contamination and direct sunlight. Keep away from fire sources and corrosive substances. Use the bag as soon as it is opened. The shelf life is no more than 24 months from the production date.

- Custom specifications are available, including

- Higher purity

- More sizes

- More shapes

- Customizable bonding

- Cautions

- This product is not classified as hazardous under applicable regulations. Dust generated during handling, machining, or surface treatment may cause mechanical irritation to the eyes and respiratory tract. Avoid inhalation of dust and use appropriate personal protective equipment during processing. Customers are advised to provide their intended application before purchase to ensure suitable product selection.

- Disclaimer

- The information provided herein is for reference only and represents typical data, not guaranteed minimum or maximum specification values. It should not be used as a basis for final product design or specific application decisions. All data are subject to change without prior notice.

- We make no warranties, express or implied, regarding the accuracy or completeness of the information. Actual properties of individual batches may vary. Users are responsible for verifying the suitability of the product for their specific applications.